## Slide 1: Analysis HXN, March 2018
CdTe system

## Slide 2: Rocking curve
Scanid: [45193:1:45233]
  Excel lab book, line 135
Angles:
  th_start = 81.25;
  th_end = 83.75;
XRF channel = 7 (Cu fluorescence channel); used for the alignment of the fluorescence map

## Slide 3
Assimetry in rocking curve and shift in the map’s columns comes from drift of grain during rock scan

## Slide 4: Shift applied in each map of the rocking curve
shift starts to be problematic

## Slide 5: Identification of the ROI in the real space where the rocking curve is complete
row 19
Rocking curve in pixel (19,20)
Rocking curve in pixel (19,30)
pixel(19,20)
pixel(19,30)

## Slide 6: Rocking curve 1
Scanid: [45193:1:45233]
  Excel lab book, line 135
Angles:
  th_start = 81.25;
  th_end = 83.75;
XRF channel = Det1_Cu (Cu fluorescence channel); used for the alignment of the fluorescence map
PC channel = sclr1_ch3

## Slide 7
2D maps corresponds to the angles in the rocking curve under the shaded area

## Slide 8: Rocking curve 7
Scanid [45477:1:45487 45449:1:45459 45460:1:45470]
  Excel lab book, line 385 - 390
Angles:
  th_start = 83.6;
  th_end = 85.08;
XRF channel = Det1_Cu (Cu fluorescence channel); used for the alignment of the fluorescence map
PC channel = sclr1_ch3

## Slide 10: Transition:
Line 407:
  move to a new area, decide to take an initial xbic measurement and then just stop xbic measurements from there on. Since they degrade too quickly in the beam

## Slide 11: Rocking curve 9
Scanid: [45526:1:45546]
  Excel lab book, line 461
Angles:
  th_start = 83.43;
  th_end = 84.43;
XRF channel = Det1_Cu (Cu fluorescence channel); used for the alignment of the fluorescence map
PC channel = sclr1_ch3

## Slide 13: Rocking curve 10
Scanid: [45547:1:45567]
  Excel lab book, line 465
Angles:
  th_start = 83.45;
  th_end = 84.45;
XRF channel = Det1_Cu (Cu fluorescence channel); used for the alignment of the fluorescence map
PC channel = sclr1_ch3

## Slide 15: Rocking curve 11
Scanid: [45569:1:45629]
  Excel lab book, line 471
Angles:
  th_start = 81.78;
  th_end = 84.78;
XRF channel = Det1_Cu (Cu fluorescence channel); used for the alignment of the fluorescence map
PC channel = sclr1_ch3

## Slide 17: Rocking curve 12
Scanid [45640:1:45650]
  Excel lab book, line 495
Angles:
  th_start = 81.61;
  th_end = 82.61;
XRF channel = Det1_Cu (Cu fluorescence channel); used for the alignment of the fluorescence map
PC channel = sclr1_ch3