## Slide 1: Analysis HXN, March 2018
CdTe system

## Slide 2: Outline
HXN convention
Geometry of the experiment
Effect of strain and tilt in the position of the Bragg peak
Results:
  Rocking curve 1
    To do: realign the diffraction maps and check the effect on the strain and tilt
  Rocking curve 7:
    To do: choose a better mask and redo the analysis
  Rocking curve 9-10
    Analysis of data: how to extract strain and tilt maps from a rocking curve
  Rocking curve 11
    Analysis of data: effect of alignement in the strain and tilt maps
  Rocking curve 12

## Slide 3: HXN conventions
Mounting of the sample:
  zero of th_motor is perpendicular to the sample:
  example: th_motor value of 82 deg in the log book, corresponds to a rocking angle of 90 – 82 deg
th_motor = 0 -> direct beam
th_motor = 82 deg/ th_rock = 90- 82 deg

## Slide 4: HXN geometry
Assumptions:
  When deg, the sample plane is perpendicular to the beam, the x axis is inboard, the y axis is upwards and z is along the beam
  motor is right handed
  Piezoscanners are on top of rotation stage
Sample at deg
Incident beam
z
x
y
Sample at deg,
z = z1
Incident beam
z
x
y
Sample at deg,
z = z2>z1 (movement of sample along z corresponds to a movement in the sample plane long x of )
Incident beam
z
x
y
Top view
Sample

## Slide 5: Geometry of the scattering
rows
columns
theta
QBragg
z
x
y
sample frame
Incoming beam
detector
Outgoing beam

## Slide 6: Effect of strain and tilt on the Bragg peak centroid position
radial
QBragg
Strain: displacement of planes along z produces Qradial
z
x
y
sample frame
out-of-plane
QBragg
Tilt of planes around y produces Qout-of-plane
z
x
y
azhimutal
z
x
y
Tilt of planes around x produces Qazhimutal
QBragg
Combination of strain and tilt produces a 3D vector
radial
azhimutal
out-of-plane
Qcentroid
Qcentroid (Qrad,Qazhi, Qout)

## Slide 7: Calculation of the centroids
Row and column centroids
y real space (pixels)
x real space (pixels)
x
y
where (x,y) are pixels in the ccd (i.e. in reciprocal space) and P(x,y,theta) is the diffracted intensity in each pixel of the ccd at given theta angle

## Slide 8: Centroid maps:
Calculation of the Xcentroid and Ycentroid for each pixel of the real space map provides a 2D map in real space
y real space (pixels)
x real space (pixels)
(Xcentroid,Ycentroid)

## Slide 9: Xcentroids and Ycentroids are converted to radial components and to Strain maps
strain
rows
columns
theta
displacement of planes along (111)
z
x
y
detector frame
sample frame
Qcentroid
Strain:
degrees
average d_space
strained d_space

## Slide 10: Xcentroids and Ycentroids are also converted in azhimutal tilt
degrees
degrees
Tilt: = azhimutal component – mean value of azhimutal

## Slide 11: Rocking curve centroid are converted in out-of-plane tilt
degrees
Tilt: = ThCentroid – mean value of Thcentroid
Thcentroid
degrees

## Slide 12: The two tilts are the two components of the total tilt around the mean tilt value
degrees
Thcentroid
degrees
degrees
tilt_total = sqrt(tilt_around_x^2 + tilt_around_y^2)
(Xcentroid,Ycentroid)
X
y
degrees
theta (degrees)

## Slide 13: Summary of Maps of the Bragg peak centroid position of rock curve 9-10 combined
ccd pixel vertical
x real space (pixels)
y real space (pixels)
ccd pixel horizontal
x real space (pixels)
y real space (pixels)
angle (deg)
x real space (pixels)
y real space (pixels)
y real space (pixels)
x real space (pixels)

## Slide 14
displacement of planes along (111)
strain
Summary of Maps of strain, tilt and XBIC!!! of rock curve 9-10 combined
total tilt (degrees)
XBIC maps

## Slide 15: Lattice spacing along 112 direction
Looking for lattice spacing maps, and its correlation with the shape of the grain and the concentration of Cd and Te
Calculation of contours of lattice spacing using the diffraction intensity as a weighted sum:
60 -70 %
1 – 2 %
6 – 7 %
10 – 20 %
60 -70 %
1 – 2 %
6 – 7 %
10 – 20 %

## Slide 16: Lattice spacing versus contours of diffracted intensity
Grain 1
Grain 7
Grain 9/10
Grain 11
Grain 12
Color code:
1 – 2%
6 – 7 %
10 – 20 %
60 – 70 %

## Slide 17: Total tilt